## Slide 1: Models of Failure and Phase Transitions in Strong Ceramics under Intense Shock Loading
The 4th International Conference on Material Strength and Applied Mechanics (MSAM 2021)
Dr. Sergey Dyachkov, Dr. Sergey Grigoryev
VNIIA
ROSATOM
Dukhov Research Institute of Automatics (VNIIA)
Moscow, Russia

## Slide 2: Outline
Motivation
development of robust and accurate model of ceramic materials response to shock compression in predictive CFD simulations
VNIIA
ROSATOM
Plate impact tests description
Ceramics failure model formulation
Obtaining best model parameters
Simulation results

## Slide 3: Uniaxial shock compression tests
*T. J. Vogler, W. D. Reinhart, L. C. Chhabildas, Journal of Applied Physics 95, 4173 (2004)
Measured wave profiles (VISAR)
Impactor and target are of ceramics under study.
Some tests include light or heavy backer material. Target is followed by a transparent LiF window.
Velocity of the ceramics/LiF interface is measured via the velocity interferometer (VISAR).
Experiment setup*
VNIIA
ROSATOM

## Slide 4: Simulation setup and reference data
Experiments
Boron carbide (B4C): no structural phase transitions, localized amorphization as a result of material failure (strength degradation)
Silicon carbide (SiC), aluminum nitride (AlN): phase transitions (structural changes in the material bulk) accompanied by strength degradation
VNIIA
ROSATOM
Simulation methods
1D finite element method (FEM) for model parameters fitting
3D smoothed particle hydrodynamics (SPH) method for validation
D. E. Grady and R. L. Moody, Tech. Rep. SAND96-0551 (Sandia National Laboratories, 1996)
T. Vogler, W. Reinhart, L. Chhabildas, J. Appl. Phys. 95 4173 (2004)
T. Vogler, W. Reinhart, L. Chhabildas, and D. Dandekar, J. Appl. Phys. 99 023512 (2006)

## Slide 5: Failure: abrupt change of strength
*G. R. Johnson, T. J. Holmquist, Journal of Applied Physics 85, 8060 (1999)
Damage accumulation:
Plastic strain
of completely
failed material
Plastic strain
increment
if :
Deviatoric stress
adjustment:
von Mises yield
criterion
Johnson-Holmquist (JH-2) model* with damage kinetics
Limiting shear strength:
VNIIA
ROSATOM

## Slide 6: Explicit numerical algorithm
S. A. Dyachkov et al., Journal of Applied Physics 124 085902 (2018)
How to evaluate ?
Wilkins:
before adjusting
shear modulus
JH - approximation:
Consistent approach:
How to evaluate ?
after
adjusting
The new numerical scheme of damage accumulation is proposed
Consistent definition for the total failure strain
Damage integration follows path 3 (instead of path 2 for JH-2)
The length and shape of the failure shock front agrees with experiments
VNIIA
ROSATOM

## Slide 7: SPH simulation with high resolution
A. N. Parshikov, S. A. Medin. J. Comp. Phys. 180 353-382 (2002)
Function approximation with smoothing kernel
SPH: approximation of Navier-Stokes equations
Riemann problem solution with strength
Simulation of uniaxial compression of boron carbide
impactor B4C
target B4C
window LiF
VNIIA
ROSATOM
Experiment BC5: D. E. Grady and R. L. Moody, Tech.Rep. SAND96-0551 (1996)
Simulation: S. A. Dyachkov et al., Journal of Applied Physics 124 085902 (2018)

## Slide 8: Model parameters fitting
VNIIA
ROSATOM
Objective function minimization
Given a set of digitized points of experimental wave profiles:
Given a set of parameters to optimize:
Each 1D FEM simulation provides a wave profile:
By reducing error | | we obtain optimal wave profile

## Slide 9: Boron Carbide

## Slide 10: JH simulation* of Grady et al. tests**
*G. R. Johnson, T. J. Holmquist, Journal of Applied Physics 85, 8060 (1999)
**D. E. Grady and R. L. Moody, Tech. Report SAND96-0551 (1996)
VNIIA
ROSATOM

## Slide 11: JH simulation* of Vogler et al. tests**
*T. J. Holmquist, G. R. Johnson, Journal of Applied Physics 100, 093525 (2006)
**T. J. Vogler, W. D. Reinhart, L. C. Chhabildas, Journal of Applied Physics 95, 4173 (2004)
Johnson-Holmquist-Beissel (JHB) model with kinetics and phase transitions
Problems:
JHB for B4C contains 26 parameters
Structural phase transition in a region between 30-40 GPa is questionable
Numerical algorithm has lack of details
VNIIA
ROSATOM

## Slide 12: Updating B4C equation of state*
*P. Dera et al., Journal of Solid State Chemistry 215 85-93 (2014)
Mie-Grüneisen approximation
Local material “bulking” as a result of shear stress induced amorphization:
Elastic energy loss during failure process
produces pressure surplus:
Total pressure:
– bulk modulus,
Mingwei Chen et al.
Science 299, 1563 (2003)
Localized shear bands in simulations
B4C amorphization under shock compression
VNIIA
ROSATOM

## Slide 13: Simulation of Vogler et al. tests*
*Vogler T. et al. J. Appl. Phys. 95, 8, 4173–4183 (2004)
Model: S. A. Dyachkov et al., Journal of Applied Physics 124 085902 (2018)
All tests are simulated using a unique set of model parameters
Simulations agree with experiments in wide range of loading regimes
Release experiments
Reshock experiments
VNIIA
ROSATOM

## Slide 14: Simulation of Grady et al. tests*
All tests of Grady et al. are better described when is reduced compared to Vogler et al. tests
BC5 test with adjusted for Vogler et al. tests provides an essentially different wave profile
VNIIA
ROSATOM
*D. E. Grady and R. L. Moody, Tech.Rep. SAND96-0551 (1996)
Model: S. A. Dyachkov et al., Journal of Applied Physics 124 085902 (2018)

## Slide 15: Failed material strength effects
Boron carbide samples manufactured via different technology provide various response
Simulations demonstrate that material response is affected much by
By fitting for a specific manufacturing technology one may obtain a good agreement between simulations and experiments with uniaxial shock compression
Strength of B4C may vary in samples
Wave profiles in two kinds of B4C samples
VNIIA
ROSATOM
Vogler T. et al. J. Appl. Phys. 95, 8, 4173–4183 (2004)
D. E. Grady and R. L. Moody, Tech.Rep. SAND96-0551 (1996)
Model: S. A. Dyachkov et al., Journal of Applied Physics 124 085902 (2018)

## Slide 16: Aluminum Nitride

## Slide 17: Aluminum nitride (AlN)
G. R. Johnson and T. J. Holmquist, Journal of Applied Physics 94, 1639 (2003)
Structural phase transition effect on wave profiles is taken into account
Hysteresis should be included to the model for the proper release profile
Equation of state
Strength properties
VNIIA
ROSATOM

## Slide 18: Aluminum nitride (AlN)
Agreement is achieved for different samples
VNIIA
ROSATOM

## Slide 19: Aluminum nitride (AlN)
G. R. Johnson and T. J. Holmquist, Journal of Applied Physics 94, 1639 (2003)
Phase transition effect
Hysteresis effect
Phase transition reduces the wave amplitude providing agreement with experiments
Reverse phase transition should begin at lower amplitude than direct one (hysteresis) which affects the release wave
VNIIA
ROSATOM

## Slide 20: Silicon carbide

## Slide 21: Silicon carbide (SiC)
Second phase should be included to the model, however lack of experiments exist to calibrate reference pressure curve
Hysteresis: 100 GPa for the direct phase transition, 35 GPa for the reverse
Phase transition with hysteresis
Strength properties
VNIIA
ROSATOM

## Slide 22: Silicon carbide (SiC)
R. Feng, G. Raiser, and Y. Gupta, Journal of applied physics 83 , 79 (1998)
Taking phase transition into account results in a correct shock wave amplitude (plateau)
Both release and reshock (with heavy backer) experiments are reproduced well
Release experiment
Reshock experiment
VNIIA
ROSATOM

## Slide 23: Silicon carbide (SiC)
T. Vogler, W. Reinhart, L. Chhabildas, and D. Dandekar, 99 Journal of applied physics, 023512 (2006)
VNIIA
ROSATOM
Release experiments
Reshock experiments
Both release and reshock tests by Vogler et al. (2006) are reproduced well

## Slide 24: Conclusion
e-mail: sergei.dyachkov@phystech.edu
B4C, AlN and SiC models are developed for simulations of intense shock shock loading up to 100 GPa
An explicit numerical algorithm is proposed for shear stress and damage evaluation during shock loading
An optimization algorithm is proposed for model parameters evaluation
Boron carbide samples produced via different manufacturing technology may have different strength after failure
Phase transitions and hysteresis should be included to the model for AlN and SiC simulations
VNIIA
ROSATOM